Circular solar: Evaluating the profitability of a photovoltaic panel recycling plant

Idiano D’Adamo1, Nicolò M. Ippolito2, Francesco Ferella2, Massimo Gastaldi2,* and Paolo Rosa3

- Department of Computer, Control and Management Engineering, Sapienza University of Rome, Via Ariosto 25, 00185 Roma, Italy

- Department of Industrial and Information Engineering and Economics, University of L’Aquila, Monteluco di Roio, 67100 L’Aquila, Italy

- Department of Management, Economics and Industrial Engineering, Politecnico di Milano, Piazza L. da Vinci 32, 20133 Milano, Italy

* Corresponding author (massimo.gastaldi@univaq.it)

Abstract

Photovoltaic (PV) panels have a crucial role in coping with the global warming mitigation and the energetic crisis currently affecting the European Community. However, from the circular perspective of end-of-life (EoL) management, there are still big issues to be solved in order to recover materials from this kind of e-wastes. Because of several reasons (e.g. type of embedded materials, illegal shipments, location of manufacturers) EoL businesses do not have the interest in approaching them. This poses a significant environmental concern in terms of their management. This work wants to assess the profitability of a specific PV module recycling plant, by evaluating several market contexts in which multiple scenarios of material price, investment and process costs will be considered. The results for a 3000 tons plant show that profitability is not verified in the absence of an avoided landfill cost. Instead, when a value of 200 €/ton is applied, the NPV is positive in 35.2% of the scenarios and at 87.6% when a value of 350 €/ton is considered. The policy choice of this value requires linking the PV module disposal fee to the circular benefits associated with its recovery.

Keywords: circular economy; economic analysis; photovoltaic; policy implications; recycling; sustainability

Introduction

The development of sustainable manufacturing models is necessarily linked to energy production (European Commission, 2020c). An increasing power generation from renewable resources like sun, biomasses, and water certainly contributes to the transition from a fossil fuel economy to a renewable energy economy (European Commission, 2020b; Giannetti et al., 2020). Global warming is the most severe threat that humankind has to face shortly (Biermann et al., 2022), and the reduction of fossil fuels that generate greenhouse emissions cannot be postponed anymore (Adedoyin et al., 2022; Caferra et al., 2021; Calabrese et al., 2021). Stakeholders' engagement (Hristov and Appolloni, 2022) and environmental education (Eliades et al., 2022) are enabling factors for this transition (European Commission, 2020a). The European Green Deal is a response to these challenges. It is a new growth strategy that aims to transform the EU into a fair and prosperous society, with a modern, resource-efficient and competitive economy where there are no net emissions of greenhouse gases in 2050 and where economic growth is decoupled from resource use (European Commission, 2019).

Photovoltaic (PV) energy plays a crucial role in this regard (D’Adamo, Gastaldi, Morone, et al., 2022). PV plants are the main example of distributed production, a concept that will revolutionize the way in which energy is generated and used in the territory. The utilization of large and flat industrial areas and building roofs can certainly drive the expansion process (Aronescu and Appelbaum, 2017).

Such an industrial model, coupled with the promotion of a circular economy approach, shall also be fostered and sustained in developing countries in order not to repeat the errors of the western countries (Abbasi et al., 2022). PV small plants to power mini-grids is an efficient way to bring electricity access to people living far from power transmission networks, particularly in developing countries with excellent solar irradiation (IRENA, 2020).

A record-breaking 175 GW of newly installed PV capacity was added in 2021, bringing the total historical value up to 942 GW. With 54.9 GW, China dominated the world in newly installed PV capacity in 2021, followed by the United States (26.9 GW) and the European Union (26.8 GW) - (International Energy Agency, 2022).

PVs are electronic devices that convert sunlight directly into electricity. The production of PV panels strictly depends on the availability of particular chemical elements such as silicon (Si), silver (Ag), gallium (Ga), indium (In), and germanium (Ge). Furthermore, we have other elements as aluminum (Al), copper (Cu), lead (Pb) and zinc (Zn) - (Azeumo et al., 2019; D’Adamo et al., 2017). PV plants are inserted within waste from electrical and electronic equipment (WEEE) - (Włodarczyk, 2022). The amount of WEEEs is indeed expected to grow exponentially in the following years, and this poses a significant environmental concern in the management (Khoshand et al., 2022). Wrong recycling procedures, illegal disposal, and non-authorized transportation to third-world countries represent the most important concerns (Awasthi et al., 2016; Fthenakis, 2000). Besides that, another threat will also affect the PV panel market in the future: the availability of the raw materials and the location of most of the PV panel manufacturing factories. China indeed hosts the majority of such plants. Considering the geopolitical instability, developing the required production chains and infrastructures is necessary to lower the foreign dependence.

There are different PV modules according to the solar cell and, once exhausted, they are classified as WEEE in the European Union. End-of-life (EoL) PV panels are usually labeled with code 160214 or 160213* if containing hazardous heavy metals such as the cadmium-telluride cells that also contain copper and tin, according to the European Waste Catalogue (Marwede and Reller, 2014; Sinha, 2013). PV modules based on mono-crystalline and poly-crystalline silicon cells do not contain hazardous heavy metals and represent 90% of the market share, whereas the remaining 10% accounts for thin film technology cells based on cadmium telluride (CdTe), copper-indium-gallium-selenide (CIGS), and amorphous silicon (Azeumo et al., 2019).

Some estimates predict that more than 78 million tons of EOL photovoltaic modules will be reached by 2050 (Tan et al., 2022). The issue of PV module recycling is increasingly urgent. If they are not properly managed, they have the potential to: i) damage our terrestrial ecology; ii) inadvertently stimulate further resource extraction and mining; and iii) reduce the net environmental benefit of solar energy harvesting (Tan et al., 2022). In this picture, the growth of PV systems has a significant increasing trend and will play a decisive role within energy models based on renewables and sustainable communities (D’Adamo, Gastaldi and Morone, 2022). The full view of sustainability requires assessing what will happen at the end of the life cycle of these products, and therefore this work focuses on the recycling of PV modules. In fact, EoL PV must be framed within a comprehensive waste management perspective (Papamichael et al., 2022; Zorpas et al., 2021). The development scenario should include optimization of the transportation of these wastes (Molano et al., 2022; Oteng et al., 2022). This highlights the need for small and medium-sized plants as well.

Several works highlights the relevance of the topic (Chatziparaskeva et al., 2022; Papamichael et al., 2022) and the need to conduct economic analyses (Rathore and Panwar, 2021) aiming to reach circular economy goals (Papamichael and Zorpas, 2022). The approach to be used is to propose technical evaluations (Dobra et al., 2021) to be applied to established economic models of analysis (D’Adamo et al., 2017). This work will assess the profitability of a polycrystalline PV module recycling plant by evaluating different market contexts in which multiple scenarios of material price, investment and process costs will be considered and finally the analysis will also address the relevance of the avoided landfill cost.

Literature analysis

Few research groups have been studying more efficient ways to recycle PV panels since 2000, in particular, to recover metals contained therein (Dias et al., 2016; Tao and Yu, 2015). Life cycle assessment of recycling was also investigated, demonstrating that such a process generates 370 kgCO2eq and requires 2780 MJ for recycling 1000 kg of PV waste. The main impacts are due to the incineration of the panel's encapsulation layers, followed by the treatments to recover silicon, copper, silver, and aluminum (Latunussa et al., 2016). Entrapment of solar cells in cementitious matrices like concrete guard rails was proposed, but the mechanical properties were not satisfactory (Fernández et al., 2011). Hence, there are two main routes to treat EoL PV modules so far, and they are the hydrometallurgical and thermal ones (Rocchetti and Beolchini, 2015).

Well-established businesses already recycle spent PV panels at the industrial level. Ethylene-vinyl acetate (EVA) is a very adhesive glue that has to be removed to disassemble the different layers of the panels. For this reason, a thermal treatment is usually proposed up to 600°C (Azeumo et al., 2019). The aluminum frame, glass, and solar cells undergo specific treatments that are proprietary and are unknown due to undisclosed business proprietary data. The main recycling stages foreseen by the current industrial processes are well described in (Marwede and Reller, 2014), in which economic considerations also are addressed regarding the profitability of the recycling. The organic solvent leaching is a stage used in most of the recycling processes currently established (Doi et al., 2001), eventually assisted by ultrasonic irradiation that makes the dissolution of EVA greater and faster (Kim and Lee, 2012).

Pagnanelli et al. (2017) tested a recycling process applied to Si-based and CdTe panels. It involves a 3-stage crushing, followed by thermal treatment and thus the final chemical process. Three fractions are obtained from crushing: a coarse fraction (>1 mm) requiring thermal treatment to remove EVA-glued layers in the glass scraps, an intermediate fraction (0.4-1 mm) of good quality glass (17% wt), and a fine fraction (<0.4 mm) that is leached to dissolve metals and thus to obtain another valuable glass fraction. The 0.08–0.4 mm fraction mainly contains Fe, Al, and Zn, while precious and hazardous metals (Ag, Ti, Te, Cu, and Cd) are concentrated in fractions <0.08 mm. Acid leaching of 0.08–0.4 mm fractions allowed them to get a third recoverable glass fraction (22%w/w). The process route can get an overall recycling rate of 91%.

Another proposed process for Si-based panels  includes the typical mechanical dismantling and pre-treatments; thus, the cells are leached with a hot 30% wt KOH aqueous solution for removing the aluminum coating and the HNO3/HF/CH3COOH/Br2 mixture for removing the silver layer (Radziemska et al., 2009). One integrated process based on flotation stages to concentrate the metals of interest was proposed by Berger et al. (2010).

Other authors focused on the recovery of pure silicon; Kang et al. (2012) recovered silicon with a 99.9% grade with a yield of 86% of the initial mass. This process includes leaching with an organic solvent, a thermal treatment at 600°C, and a final leaching stage with acids. Silver is the most precious metal contained in Si-based PV modules. After milling, sieving, pyrolysis at 500 °C was applied and the resulting material leached in HNO3/NaCl: the silver extraction yield was 92% (Dias et al., 2016).

Other authors proposed the recycling of the cells for producing new solar cells instead of recovering the different materials and metals. For instance, Lee et al. (2017) proposed a recycling process to produce crystalline silicon (c-Si) solar cells using a Si wafer reclaimed from exhausted cells. The efficiency of the new cell was encouraging, being 17.6%. Another remanufacturing process was studied to recover silicon wafers from EoL solar panels and produce secondary cells with a conversion efficiency between 15 and 16.0% (Shin et al., 2017).

The literature places strong emphasis on the mix among the boards to be treated (Rosa and Terzi, 2016) in order to identify the correct technological process to improve performance (Zueva et al., 2021) and denotes the relevance of economic aspects in EoL management (D’Adamo and Rosa, 2019). This goal requires optimizing the disassembly process (Sassanelli et al., 2021), improving the decision-making process (Luglietti et al., 2016) and the circularity of resources within manufacturing context (Acerbi et al., 2022), in order to increase green supply chain management (Sathiya et al., 2021) minimizing the level of emissions (Cucchiella et al., 2017), and maximizing gold recovery (Ippolito et al., 2021). The literature highlights how the circular approach is essential to sustainability goals (Qazi and Appolloni, 2022), also within solar projects (Van Opstal and Smeets, 2023). Circular management of solar resources in all countries is called to have a perspective that looks at the long term and not the short term (Chowdhury et al., 2020; Tasnim et al., 2022).

Description of the recycling process

The technical analysis is based on a recycling process studied at the University of La Sapienza Rome, whose main results are reported in (Azeumo et al., 2019). EoL polycrystalline-silicon PV panels were treated by applying a physic mechanical and chemical treatment. The module was manually dismantled to remove the aluminum frame; cables and junction boxes were also detached. The panel was cut into 130x130 mm plates undergoing mechanical treatments.

First, the plates were crushed with a knife mill until reaching the cut-off of the grid installed beneath, i.e., 2, 1, and 0.4 cm, according to the different trials carried out (Azeumo, 2020). The resulting material was composed of glass and metals. This fraction underwent dense medium separation, a typical technique of the mining industry, using aqueous solutions with additives like sodium chloride and sodium polytungstate.

The two fractions were thus separated, i.e., the float (silicon fine powder and EVA) and the sink (metals, glass, and a small amount of EVA and silicon). The latter was washed with water, dried in the oven, ground by a ring mill, and sieved. The fractions obtained were quantified and characterized by Inductively Coupled Plasma-Mass Spectrometry (ICP-MS) after acid digestion with aqua regia.

The chemical treatment aims to remove EVA by dissolving it in a suitable solvent. The PV pieces underwent a thermal pre-treatment at 190°C for 2 h. Thus, different boiling solvents were tested in the leaching step, enhanced by ultrasounds, for 2 h. This stage is crucial for the detachment of the different layers and, thus, their separation and recovery. The overall mass composition of the recovered materials for a polycrystalline PV panel is distributed as follows: plastic 9.93 (% wt), metals 1.37 (% wt), glass 84.02 (% wt) and other metals 0.71 (% wt) - (Azeumo, 2020).

The metal fraction was mainly composed of ribbons that connect the various cells. The fraction "others" includes especially EVA and silicon. Furthermore, the material balance does not close to 100%: this is due to the inevitable losses during each phase, in particular, crushing and milling/sieving. The total loss accounts for nearly 3.97% wt of the total mass. The most concentrated metals detected in the metallic fraction were Cu 77.11% wt, Ag 0.54%, Pb 3.14%, and Zn 0.19%. Metallic ribbons consist mainly of copper coatings with a thin layer of silver. There are also lead and zinc in smaller quantities. After the experimental campaign, a recycling process, whose block diagram is shown in Figure 1, was thus designed.

Please insert Figure 1

Materials and methods

The size of the PV module recycling plant significantly influences its profitability. Some works show that for 10,000 tonnes/year plants it is not verified (Mahmoudi et al., 2020) and other works set the minimum value at 20,000 tonnes/year (Choi and Fthenakis, 2014; Deng et al., 2019). In these scenarios, it is evident how the revenues obtained from the materials do not offset the related investment and operating costs, in the absence of an environmental contribution associated with the recovery of these wastes. However, considering this variable, the scenario may change: some works propose verified profitability for plants smaller than 4000 tonnes/year (Dias et al., 2022), others point out that it is not verified for 2000 tonnes/year (D’Adamo et al., 2017). This work considers the scenario in which 3000 tonnes/year are recovered. It is worth specifying that typically 1 MW of PV systems produce about 75 tonnes of waste (Choi and Fthenakis, 2014). Thus, the plant considered in this work can recover 40 MW.

The discounted cash flow (DCF) method is used to evaluate the economic profitability of a recycling plant. Specifically, net present value (NPV) is the chosen indicator that can consider both the time value of money and include the various estimated cash flows (Woo and Whale, 2022). It is a prediction of what might happen in the future but is still important as it highlights whether a market has economic potential or not. The following economic model is used in this work (D’Adamo et al., 2017):

| NPV=DCI-DCO | (1) |
| --- | --- |
| DCI=t=1N(mAlm*yAl*plAl*prAl,t*S+mglassm*yglass*plglass*prglass,t*S+mSim*ySi*plSi*prSi,t*S+mCum*yCu*plCu*prCu,t*S+mAgm*yAg*plAg*prAl,t*S+mZnm*yZn*plZn*prZn,t*S)/1+rt+t=1N(ACPM,t*S)/1+rt | (2) |
| DCO=t=0Ndebt-1((Cinvu*S)/Ndebt+Cinvu*S-Clcs,t*rd)/1+rt+t=1N(Cpu*S+Ccu*S+mmm*CCM,tu*S+ebtt*Ctaxu)/1+rt | (3) |

On the discounted cash inflows (DCI) side, an important role is related to the recycling of materials contained in the products being processed. Therefore, the amount of materials recovered is multiplied with some variables such as the market price of these materials but also their recycling rate and degree of purity (Choi and Fthenakis, 2014). With regard to the prices of recycled materials, the main websites devoted to these topics were considered (Heraeus, Kme, Investing). Therefore, from the market analysis, it is found that among the materials that can be recovered from the recycling of PV modules, silver is the most valuable component. Its average value is quantified as 650 €/kg, while the lowest value is associated with glass (0.125 €/kg). Furthermore, we identify 2.3 €/kg for Al, 2.1 €/kg for Si, 8.5 €/kg for Cu and 3.1 €/kg for Zn. These values are higher than in previous analyses, but the result was expected given the current surge in the raw materials market (D’Adamo et al., 2017). Regarding the level of purity an optimistic scenario is considered, set equal to 100% although this condition is not always verified (Choi and Fthenakis, 2014). Regarding, yield of recycled material, values emerged in the literature were considered, where again a very satisfactory recovery perspective emerges (Deng et al., 2019).

To this item can be added a cost that is not incurred. Within a business plan, this item can be considered as revenue if the PV producers are also recyclers (McDonald and Pearce, 2010). Alternatively, recycling centres receive such a fee for disposing of PV modules appropriately. The literature proposes several values: 112 $/t (Gautam et al., 2022), 500 $/t  (Rubino et al., 2020) and 225-425 $/t (Granata et al., 2022).

The analysis of discounted cash outflows (DCO) turns out to be characterized by high variability. As for investment costs, they are influenced by the size of the plant and some work shows that they can play a significant role on the profitability of the investment (Mahmoudi et al., 2020). Turning to an analysis of operating costs, several components emerge. Production process costs turn out to be the value that per unit ton represents the greatest value (Cucchiella et al., 2015), however there is a significant increase in the cost of collection/transportation when analysing a large target area (Choi and Fthenakis, 2014; Gautam et al., 2022). In addition, some materials that cannot be recycled (plastics) must be properly disposed of in suitable locations. In order to identify comparable values in the literature the following data are proposed related to unitary collection cost (Ccu), unitary conferred materials cost (Ccmu), unitary process cost (Cpu) and unitary investment cost (Cinvu): Ccu = 210 €/t; Ccmu  = 90 €/t; Cpu = 320 €/t and Cinvu = 270 €/t (D’Adamo et al., 2017) and Ccu = 288 $/t; Cpu = 351 $/t and Cinvu = 400 $/t (Gautam et al., 2022).

In addition, some assumptions should be specified: i) recovered Lead can be valued by other centres and therefore is considered to have zero value in the market exchange; ii) other metals are not included as potential revenues and iii) lost dust is also not included in the economic analysis. Finally, a conservative assumption is made in which material prices do not increase.

The two-macro variables that typically characterize a DCF are the opportunity cost of capital set at 5% and the useful life of the project set at 10 years (D’Adamo et al., 2017). In addition, 2022 is taken as year zero of the project, such that in 2023, the project goes into operation and the entire initial investment is covered by third party funds. The choice of input values was therefore made in accordance with the literature and experts in the field working in recycling centers. Table 1 proposes the list of acronyms and values of input data.

Please insert Table 1

In order to have a suitable model in multiple case studies, the map of several scenarios as a function of the baseline inputs is proposed (Figure 2):

- regarding the price of sales materials, both a pessimistic and an optimistic scenario was added in which the average value is decreased/increased by its standard deviation than baseline scenario.

- Inherently the avoided landfill cost, two values were identified that are consistent with, but not equal to, what has been proposed in the literature. The 500 €/t value was not considered, but values of 200 €/t and 350 €/t were favoured. In addition, the scenario in which this value is zero was considered. A useful scenario at the end of policy considerations.

- Finally, about costs, the two extremes were taken for all cost variables such that two related scenarios were identified. An intermediate scenario was then added.

Please insert Figure 2

Please insert Table 1

Results

The economic model used in this workr was used through a set of input data that allowed for the inclusion of variability in the input values that can characterize the input data. The number of scenarios analysed in this work amounted to twenty-seven. It is obtained from the combination of three scenarios related to costs with three scenarios associated with changes in revenues through material prices. The nine scenarios obtained from the combination of costs and revenues are then repeated for each of the three scenarios related to the potential avoided landfill cost – Table 2.

Please insert Table 2

The results show that profitability is not verified in all scenarios and, there are seventeen (about 63% of the total) scenarios in which NPV is negative. The considerations that emerge are as follows. The first sharply defines that in the absence of an economic contribution that enhances the environmental damage avoided through the receipt of a fee to dispose of PV modules appropriately, the NPV is always negative. This result influences the policy maker because the use of renewables has a clear support for combating climate change, quantifiable as 620 gCO2eq/kWh (D’Adamo et al., 2021); however, sustainability requires the evaluation of a product throughout its life cycle. Energy pay-back time for silicon panels is quantified as 2.6 years, which can be reduced to 1.6 years by including the recycling process (Vellini et al., 2017). The second consideration is inherent to a scenario in which the variables present a high value of costs, since in such a situation only in one scenario the NPV is positive and equal to 1292 k€ (when considering a Price optimistic scenario and a High avoided cost of landfill). This inevitably drives the consideration that costs must follow innovation processes that lead them to have high performance values by recovering all possible materials from a waste, giving them the opportunity to be a benefit but at the same time, technological development must also lead to cost reduction. Some analyses confirm the unprofitability of the recycling plants, but the cost to recycle could be as little as 0.03 $/kg (Faircloth et al., 2019).

Potential synergies emerge from combining PV within other products for recycling (Islam et al., 2020). In addition, there is greater interest in thin film modules consider the presence of higher value-added critical materials (Choi and Fthenakis, 2010; Cucchiella et al., 2015). When considering the intermediate cost scenario if it is true that in the presence of a High avoided cost of landfill the NPV is always positive, on the other hand it is noted that this performance remains only verified in the Price optimistic scenario if the avoided cost of landfill is reduced from 350 to 200 €/t. The third consideration relates to prices since while it is true that in an economic situation in which the raw materials market is affected by strong fluctuations, the comparison among contexts shows that depending on the pessimistic, baseline and optimistic scenario there are two, three and five scenarios in which NPV is positive, respectively. The most striking finding, however, is the change in the profits that can be realized (about a 1515 k€ increase between the different scenarios). This value is motivated by the low presence of valuable materials that are recorded within the polycrystalline modules. The positive NPV ranges from 5 to 4781 k€. Such significant values are also recorded in other analyses, where the payback period is quantified as 1 year (Lim et al., 2022). Moreover, the profitability conditions of these recycling plants require not high levels of taxation (Liu et al., 2018), as does the level of risk with which these projects may be associated (Lim et al., 2022).

However, if the future market environment predicts continued growth in material prices, businesses can be competitive if they create partnerships or industrial symbiosis (Colpo et al., 2022) such that they have a short supply chain with access to contained raw materials. Furthermore, agreements between various stakeholders about recycling fees will further boost the overall economic viability of PV recycling (Daniela-Abigail et al., 2022). Cooperation between government and private entities is also needed, utilizing the advantages associated with adequate infrastructure and research and development programs (Yu et al., 2022).

Finally, it is necessary to promote the development of small and medium-sized plants because decentralized models involve PV plants installed within different territories (D’Adamo et al., 2017). This points to the autonomy of individual territories, and within the concept of sustainable communities these territories must be able to produce energy but also manage the waste they have produced. Where only large plants are developed, it results in transportation needed to transfer this waste, which inevitably reduces the environmental benefits associated with the use of renewables. Furthermore, particular attention is given to the recovery of valuable materials (especially Ag) which although present in smaller quantities has a much larger selling price than other materials as pointed out earlier (Granata et al., 2022). At the same time, large quantities of some materials can bring great benefits, particularly if the market for these products (e.g., glass) is heading toward growing trends (Dias et al., 2022).

In order to give robustness to the results obtained, a risk analysis was conducted, in which all critical variables analysed previously (including cost components and material selling prices) are varied by means of the Monte Carlo model. One thousand iterations of the NPV are considered and the value of the intermediate scenario is taken as the mean value, while the standard deviation is calculated based on the alternative scenarios – Figure 3. The analyses then refer to the joint Intermediate cost and Price baseline scenario according to the three distinct avoided landfill costs.

Please insert Figure 3

The results emerging from these analyses confirm previous results. In the market context in which an avoided cost of landfill of 0 €/t is applied, there are about 1.1% scenarios in which the NPV is positive. Thus, we can point out that investors have no advantage to invest in a recycling plant that only processes 3000 tons of polycrystalline PV modules. The situation becomes diametrically different when considering an avoided cost of landfill of 350 €/t since in about 87.6% of iterations, the NPV is positive. This work has the limitation of not associating the correct value of the PV module disposal fee with the relative net benefit associated with its sparing environmental management. Such a value requires environmental analyses that quantify the exact value of emission reductions, but it is also contextually linked to the economic value associated with CO2. Thus, economic analyses aim to support the policy maker in order to highlight how the profitability of a recycling plant varies according to this scenario. If an intermediate scenario between the previous two is chosen, with an avoided cost of landfill of 200 €/t, the NPV turns out to be positive in about 35.2% of the scenarios. Some authors have calculated the unitary subsidy, which is 1.95 USD/kW (Liu et al., 2018), to have a benefit-cost ratio of 1.1 (Liu et al., 2020). This value is considered a reference value for material recycling businesses.

Conclusions

PV panels have a crucial role in coping with the global warming mitigation and the energetic crisis currently affecting the European Community. However, from the perspective of EoL management, there are still big issues to be solved in order to recover materials from this kind of e-wastes. Because of several reasons (e.g. type of embedded materials, illegal shipments, location of manufacturers) EoL businesses do not have the interest in approaching them. This poses a significant environmental concern in terms of their management. This work assessed the profitability of a specific PV module recycling plant, by evaluating different market contexts in which multiple scenarios of material price, investment and process costs are considered. The results emerging from these analyses confirm what has been evidenced by other works available in the literature. Specifically, stakeholders have no advantage to invest in a recycling plant processing just 3000 tons of polycrystalline PV modules. The situation becomes diametrically different when landfill costs are avoided. NPV ranges from 5 to 4781 thousand € with a disposal fee of 300 €/ton in function of price scenario considering a low/intermediate cost scenario. Instead, NPV varies from 951 to 2696 thousand € with a disposal fee of 350 €/ton only for an optimistic price scenario considering low/intermediate cost scenario. The limit of this work lies in not associating the correct value of the PV module disposal fee with the relative net benefit associated with its sparing environmental management. Thus, further economic analyses should be done in order to better understand the influence of certain policy measures on the recovery of PV panels.

References

Abbasi KR, Hussain K, Radulescu M, et al. (2022) Asymmetric impact of renewable and non-renewable energy on the industrial sector in Pakistan: Fresh evidence from Bayesian and non-linear ARDL. Renewable Energy 187: 944–957. DOI: 10.1016/j.renene.2022.02.012.

Acerbi F, Sassanelli C and Taisch M (2022) A conceptual data model promoting data-driven circular manufacturing. Operations Management Research. DOI: 10.1007/s12063-022-00271-x.

Adedoyin FF, Erum N and Ozturk I (2022) Does higher innovation intensity matter for abating the climate crisis in the presence of economic complexities? Evidence from a Global Panel Data. Technological Forecasting and Social Change 181: 121762. DOI: 10.1016/j.techfore.2022.121762.

Aronescu A and Appelbaum J (2017) Design optimization of photovoltaic solar fields-insight and methodology. Renewable and Sustainable Energy Reviews 76: 882–893. DOI: 10.1016/j.rser.2017.03.079.

Awasthi AK, Zeng X and Li J (2016) Environmental pollution of electronic waste recycling in India: A critical review. Environmental Pollution 211: 259–270. DOI: 10.1016/j.envpol.2015.11.027.

Azeumo MF (2020) Recovery of materials contained in WEEE. Ph.D. Thesis - La Sapienza University of Rome.

Azeumo MF, Germana C, Ippolito NM, et al. (2019) Photovoltaic module recycling, a physical and a chemical recovery process. Solar Energy Materials and Solar Cells 193: 314–319. DOI: 10.1016/j.solmat.2019.01.035.

Berger W, Simon F-G, Weimann K, et al. (2010) A novel approach for the recycling of thin film photovoltaic modules. Resources, Conservation and Recycling 54(10): 711–718. DOI: 10.1016/j.resconrec.2009.12.001.

Biermann F, Hickmann T, Sénit CA, et al. (2022) Scientific evidence on the political impact of the Sustainable Development Goals. Nature Sustainability 5(9). Springer US: 795–800. DOI: 10.1038/s41893-022-00909-5.

Caferra R, Colasante A and Morone A (2021) Who Is Afraid Of The Dark? Some Evidence From A Cross-Country Investigation. Energy Sources, Part B: Economics, Planning, and Policy 16(11–12). Taylor & Francis: 1016–1025. DOI: 10.1080/15567249.2021.1909672.

Calabrese A, Costa R, Gastaldi M, et al. (2021) Implications for Sustainable Development Goals: A framework to assess company disclosure in sustainability reporting. Journal of Cleaner Production 319: 128624. DOI: 10.1016/j.jclepro.2021.128624.

Chatziparaskeva G, Papamichael I, Voukkali I, et al. (2022) End-of-Life of Composite Materials in the Framework of the Circular Economy. Microplastics 1(3): 377–392. DOI: 10.3390/microplastics1030028.

Choi J-K and Fthenakis V (2010) Economic Feasibility of Recycling Photovoltaic Modules. Journal of Industrial Ecology 14(6). John Wiley & Sons, Ltd: 947–964. DOI: 10.1111/j.1530-9290.2010.00289.x.

Choi J-K and Fthenakis V (2014) Crystalline silicon photovoltaic recycling planning: macro and micro perspectives. Journal of Cleaner Production 66. Elsevier Ltd: 443–449. DOI: 10.1016/j.jclepro.2013.11.022.

Chowdhury MS, Rahman KS, Chowdhury T, et al. (2020) An overview of solar photovoltaic panels’ end-of-life material recycling. Energy Strategy Reviews 27: 100431. DOI: 10.1016/j.esr.2019.100431.

Colpo I, Martins MES, Buzuku S, et al. (2022) Industrial symbiosis in Brazil: A systematic literature review. Waste Management & Research. SAGE Publications Ltd STM: 0734242X221084065. DOI: 10.1177/0734242X221084065.

Cucchiella F, D’Adamo I and Rosa P (2015) End-of-Life of used photovoltaic modules: A financial analysis. Renewable and Sustainable Energy Reviews 47: 552–561. DOI: 10.1016/j.rser.2015.03.076.

Cucchiella F, Gastaldi M and Miliacca M (2017) The management of greenhouse gas emissions and its effects on firm performance. Journal of Cleaner Production 167: 1387–1400. DOI: 10.1016/j.jclepro.2017.02.170.

D’Adamo I and Rosa P (2019) A Structured Literature Review on Obsolete Electric Vehicles Management Practices. Sustainability (Switzerland) 11(6876): 1–17. DOI: 10.3390/su11236876.

D’Adamo I, Miliacca M and Rosa P (2017) Economic Feasibility for Recycling of Waste Crystalline Silicon Photovoltaic Modules. International Journal of Photoenergy 2017: 1–6. DOI: 10.1155/2017/4184676.

D’Adamo I, de Monte F, Ferella F, et al. (2021) The case study of a photovoltaic plant located at the university of L’Aquila: An economic analysis. Journal of Cleaner Production 278: 123561. DOI: 10.1016/j.jclepro.2020.123561.

D’Adamo I, Gastaldi M, Morone P, et al. (2022) Economics and policy implications of residential photovoltaic systems in Italy’s developed market. Utilities Policy 79: 101437. DOI: 10.1016/j.jup.2022.101437.

D’Adamo I, Gastaldi M and Morone P (2022) Solar collective self-consumption: Economic analysis of a policy mix. Ecological Economics 199: 107480. DOI: 10.1016/j.ecolecon.2022.107480.

Daniela-Abigail H-L, Tariq R, Mekaoui A El, et al. (2022) Does recycling solar panels make this renewable resource sustainable? Evidence supported by environmental, economic, and social dimensions. Sustainable Cities and Society 77: 103539. DOI: 10.1016/j.scs.2021.103539.

Deng R, Chang NL, Zi O, et al. (2019) A techno-economic review of silicon photovoltaic module recycling. Renewable and Sustainable Energy Reviews 109. Elsevier Ltd: 532–550. DOI: 10.1016/j.rser.2019.04.020.

Dias P, Javimczik S, Benevit M, et al. (2016) Recycling WEEE: Extraction and concentration of silver from waste crystalline silicon photovoltaic modules. Waste Management 57: 220–225. DOI: 10.1016/j.wasman.2016.03.016.

Dias PR, Schmidt L, Chang NL, et al. (2022) High yield, low cost, environmentally friendly process to recycle silicon solar panels: Technical, economic and environmental feasibility assessment. Renewable and Sustainable Energy Reviews 169: 112900. DOI: 10.1016/j.rser.2022.112900.

Dobra T, Vollprecht D and Pomberger R (2021) Thermal delamination of end-of-life crystalline silicon photovoltaic modules. Waste Management & Research 40(1). SAGE Publications Ltd STM: 96–103. DOI: 10.1177/0734242X211038184.

Doi T, Tsuda I, Unagida H, et al. (2001) Experimental study on PV module recycling with organic solvent method. Solar Energy Materials and Solar Cells 67(1): 397–403. DOI: 10.1016/S0927-0248(00)00308-1.

Eliades F, Doula MK, Papamichael I, et al. (2022) Carving out a Niche in the Sustainability Confluence for Environmental Education Centers in Cyprus and Greece. Sustainability 14(14): 8368. DOI: 10.3390/su14148368.

European Commission (2019) The European Green Deal COM(2019) 640. DOI: 10.2307/j.ctvd1c6zh.7.

European Commission (2020a) A new Circular Economy Action Plan For a cleaner and more competitive Europe.

European Commission (2020b) A new Circular Economy Action Plan For a cleaner and more competitive Europe - ANNEX.

European Commission (2020c) A New Industrial Strategy for Europe COM(2020) 102. Available at: https://ec.europa.eu/info/sites/info/files/communication-eu-industrial-strategy-march-2020_en.pdf.

Faircloth CC, Wagner KH, Woodward KE, et al. (2019) The environmental and economic impacts of photovoltaic waste management in Thailand. Resources, Conservation and Recycling 143. Elsevier: 260–272. DOI: 10.1016/J.RESCONREC.2019.01.008.

Fernández LJ, Ferrer R, Aponte DF, et al. (2011) Recycling silicon solar cell waste in cement-based systems. Solar Energy Materials and Solar Cells 95(7): 1701–1706. DOI: 10.1016/j.solmat.2011.01.033.

Fthenakis VM (2000) End-of-life management and recycling of PV modules. Energy Policy 28(14): 1051–1058. DOI: 10.1016/S0301-4215(00)00091-4.

Gautam A, Shankar R and Vrat P (2022) Managing end-of-life solar photovoltaic e-waste in India: A circular economy approach. Journal of Business Research 142: 287–300. DOI: 10.1016/j.jbusres.2021.12.034.

Giannetti BF, Agostinho F, Almeida CMVB, et al. (2020) Insights on the United Nations Sustainable Development Goals scope: Are they aligned with a ‘strong’sustainable development? Journal of Cleaner Production 252. Elsevier: 119574. DOI: 10.1016/j.jclepro.2019.119574.

Granata G, Altimari P, Pagnanelli F, et al. (2022) Recycling of solar photovoltaic panels: Techno-economic assessment in waste management perspective. Journal of Cleaner Production 363: 132384. DOI: 10.1016/j.jclepro.2022.132384.

Hristov I and Appolloni A (2022) Stakeholders’ engagement in the business strategy as a key driver to increase companies’ performance: Evidence from managerial and stakeholders’ practices. Business Strategy and the Environment 31(4). John Wiley & Sons, Ltd: 1488–1503. DOI: 10.1002/bse.2965.

International Energy Agency (2022) Snapshot of Global PV Markets 2021.

Ippolito NM, Birloaga I, Ferella F, et al. (2021) Preliminary Study on Gold Recovery from High Grade E-Waste by Thiourea Leaching and Electrowinning. Minerals 11(3): 235. DOI: 10.3390/min11030235.

IRENA (2020) Global Renewables Outlook: Energy transformation 2050.

Islam MT, Nizami MSH, Mahmoudi S, et al. (2020) Reverse logistics network design for waste solar photovoltaic panels: A case study of New South Wales councils in Australia. Waste Management & Research 39(2). SAGE Publications Ltd STM: 386–395. DOI: 10.1177/0734242X20962837.

Kang S, Yoo S, Lee J, et al. (2012) Experimental investigations for recycling of silicon and glass from waste photovoltaic modules. Renewable Energy 47: 152–159. DOI: 10.1016/j.renene.2012.04.030.

Khoshand A, Karami A, Rostami G, et al. (2022) Prediction of e-waste generation: Application of modified adaptive neuro-fuzzy inference system (MANFIS). Waste Management & Research. SAGE Publications Ltd STM: 0734242X221122598. DOI: 10.1177/0734242X221122598.

Kim Y and Lee J (2012) Dissolution of ethylene vinyl acetate in crystalline silicon PV modules using ultrasonic irradiation and organic solvent. Solar Energy Materials and Solar Cells 98: 317–322. DOI: 10.1016/j.solmat.2011.11.022.

Latunussa CEL, Ardente F, Blengini GA, et al. (2016) Life Cycle Assessment of an innovative recycling process for crystalline silicon photovoltaic panels. Solar Energy Materials and Solar Cells 156: 101–111. DOI: 10.1016/j.solmat.2016.03.020.

Lee J-K, Lee J-S, Ahn Y-S, et al. (2017) Photovoltaic performance of c-Si wafer reclaimed from end-of-life solar cell using various mixing ratios of HF and HNO3. Solar Energy Materials and Solar Cells 160: 301–306. DOI: 10.1016/j.solmat.2016.10.034.

Lim MSW, He D, Tiong JSM, et al. (2022) Experimental, economic and life cycle assessments of recycling end-of-life monocrystalline silicon photovoltaic modules. Journal of Cleaner Production 340: 130796. DOI: 10.1016/j.jclepro.2022.130796.

Liu C, Zhang Q and Wang H (2020) Cost-benefit analysis of waste photovoltaic module recycling in China. Waste Management 118: 491–500. DOI: 10.1016/j.wasman.2020.08.052.

Liu J, Bai H, Liang H, et al. (2018) How to recycle the small waste household appliances in China? A revenue- expenditure analysis. Resources, Conservation and Recycling 137: 292–301. DOI: 10.1016/j.resconrec.2018.06.015.

Luglietti R, Rosa P, Terzi S, et al. (2016) Life Cycle Assessment Tool in Product Development: Environmental Requirements in Decision Making Process. Procedia CIRP 40: 202–208. DOI: 10.1016/j.procir.2016.01.103.

Mahmoudi S, Huda N and Behnia M (2020) Environmental impacts and economic feasibility of end of life photovoltaic panels in Australia: A comprehensive assessment. Journal of Cleaner Production 260: 120996. DOI: 10.1016/j.jclepro.2020.120996.

Marwede M and Reller A (2014) Estimation of Life Cycle Material Costs of Cadmium Telluride– and Copper Indium Gallium Diselenide–Photovoltaic Absorber Materials based on Life Cycle Material Flows. Journal of Industrial Ecology 18(2): 254–267. DOI: 10.1111/jiec.12108.

McDonald NC and Pearce JM (2010) Producer responsibility and recycling solar photovoltaic modules. Energy Policy 38(11): 7041–7047. DOI: 10.1016/j.enpol.2010.07.023.

Molano JC, Xing K, Majewski P, et al. (2022) A holistic reverse logistics planning framework for end-of-life PV panel collection system design. Journal of Environmental Management 317: 115331. DOI: 10.1016/j.jenvman.2022.115331.

Oteng D, Zuo J and Sharifi E (2022) Environmental emissions influencing solar photovoltaic waste management in Australia: An optimised system network of waste collection facilities. Journal of Environmental Management 314: 115007. DOI: 10.1016/j.jenvman.2022.115007.

Pagnanelli F, Moscardini E, Granata G, et al. (2017) Physical and chemical treatment of end of life panels: An integrated automatic approach viable for different photovoltaic technologies. Waste Management 59: 422–431. DOI: 10.1016/j.wasman.2016.11.011.

Papamichael I and Zorpas AA (2022) End-of-waste criteria in the framework of end-of-life PV panels concerning circular economy strategy. Waste Management & Research 40(12). SAGE Publications Ltd STM: 1677–1679. DOI: 10.1177/0734242X221132886.

Papamichael I, Voukkali I, Jeguirim M, et al. (2022) End-of-Life Management and Recycling on PV Solar Energy Production. Energies 15(17): 6430. DOI: 10.3390/en15176430.

Qazi AA and Appolloni A (2022) A systematic review on barriers and enablers toward circular procurement management. Sustainable Production and Consumption 33: 343–359. DOI: 10.1016/j.spc.2022.07.013.

Radziemska E, Ostrowski P and Seramak T (2009) Chemical treatment of crystalline silicon solar cells as a main stage of PV modules recycling. Ecological Chemistry and Engineering. S 16(3): 379–388. DOI: 10.1016/j.renene.2009.11.031.

Rathore N and Panwar NL (2021) Strategic overview of management of future solar photovoltaic panel waste generation in the Indian context. Waste Management & Research 40(5). SAGE Publications Ltd STM: 504–518. DOI: 10.1177/0734242X211003977.

Rocchetti L and Beolchini F (2015) Recovery of valuable materials from end-of-life thin-film photovoltaic panels: environmental impact assessment of different management options. Journal of Cleaner Production 89: 59–64. DOI: 10.1016/j.jclepro.2014.11.009.

Rosa P and Terzi S (2016) Comparison of current practices for a combined management of printed circuit boards from different waste streams. Journal of Cleaner Production 137. Elsevier Ltd: 300–312. DOI: 10.1016/j.jclepro.2016.07.089.

Rubino A, Granata G, Moscardini E, et al. (2020) Development and Techno-Economic Analysis of an Advanced Recycling Process for Photovoltaic Panels Enabling Polymer Separation and Recovery of Ag and Si. Energies 13(24): 6690. DOI: 10.3390/en13246690.

Sassanelli C, Rosa P and Terzi S (2021) Supporting disassembly processes through simulation tools: A systematic literature review with a focus on printed circuit boards. Journal of Manufacturing Systems 60. Elsevier: 429–448. DOI: 10.1016/J.JMSY.2021.07.009.

Sathiya V, Chinnadurai M, Ramabalan S, et al. (2021) Mobile robots and evolutionary optimization algorithms for green supply chain management in a used-car resale company. Environment, Development and Sustainability 23(6): 9110–9138. DOI: 10.1007/s10668-020-01015-2.

Shin J, Park J and Park N (2017) A method to recycle silicon wafer from end-of-life photovoltaic module and solar panels by using recycled silicon wafers. Solar Energy Materials and Solar Cells 162: 1–6. DOI: 10.1016/j.solmat.2016.12.038.

Sinha P (2013) Life cycle materials and water management for CdTe photovoltaics. Solar Energy Materials and Solar Cells 119: 271–275. DOI: 10.1016/j.solmat.2013.08.022.

Tan J, Jia S and Ramakrishna S (2022) End-of-Life Photovoltaic Modules. Energies 15(14): 5113. DOI: 10.3390/en15145113.

Tao J and Yu S (2015) Review on feasible recycling pathways and technologies of solar photovoltaic modules. Solar Energy Materials & Solar Cells 141. Elsevier: 108–124. DOI: 10.1016/j.solmat.2015.05.005.

Tasnim SS, Rahman MM, Hasan MM, et al. (2022) Current challenges and future perspectives of solar-PV cell waste in Bangladesh. Heliyon 8(2): e08970. DOI: 10.1016/j.heliyon.2022.e08970.

Van Opstal W and Smeets A (2023) Circular economy strategies as enablers for solar PV adoption in organizational market segments. Sustainable Production and Consumption 35: 40–54. DOI: 10.1016/j.spc.2022.10.019.

Vellini M, Gambini M and Prattella V (2017) Environmental impacts of PV technology throughout the life cycle: Importance of the end-of-life management for Si-panels and CdTe-panels. Energy 138: 1099–1111. DOI: 10.1016/j.energy.2017.07.031.

Włodarczyk R (2022) Analysis of the Photovoltaic Waste-Recycling Process in Polish Conditions&mdash;A Short Review. Sustainability 14(8): 4739. DOI: 10.3390/su14084739.

Woo SM and Whale J (2022) A mini-review of end-of-life management of wind turbines: Current practices and closing the circular economy gap. Waste Management & Research. SAGE Publications Ltd STM: 0734242X221105434. DOI: 10.1177/0734242X221105434.

Yu HF, Hasanuzzaman M, Rahim NA, et al. (2022) Global Challenges and Prospects of Photovoltaic Materials Disposal and Recycling: A Comprehensive Review. Sustainability 14(14): 8567. DOI: 10.3390/su14148567.

Zorpas AA, Navarro-Pedreño J, Jeguirim M, et al. (2021) Crisis in leadership vs waste management. Euro-Mediterranean Journal for Environmental Integration 6(3): 80. DOI: 10.1007/s41207-021-00284-1.

Zueva S, Ferella F, Corradini V, et al. (2021) An Effective New Treatment of Fluoride-Containing Sludge Resulting from the Manufacture of Photovoltaic Cells. Processes 9(10): 1745. DOI: 10.3390/pr9101745.