Testing and Modelling Indirectly-Supported One-Way R/C SlabsDevoid of Transverse Reinforcement

Pietro G. Gambarova1, Francesco Lo Monte2,

Riccardo Visentini3 and Mattia Zecchillo4

ABSTRACT: Small-to-medium underground facilities and provisional roofs are often covered by means of side-by-side one-way R/C slabs, whose short sides are frequently supported by means of corbels. In such a case,the net reinforcing the bottom part of the slabs is accompanied by a second net roughly placed at mid-depth to reinforce the corbels. Because of their unconspicuousness, these structures are often under-reinforced in shear, with possible severe consequences under exceptional loads. To have fresh information, six indirectly-supported one-way R/C slabs have been recently tested in Milan, and the tests of the two thickest slabs provided with straight bars(with or without hooks in the corbels) are presented.There are no major effects ensuing from the two bar arrangements, but hooks improve bond effectivenes in the tensile zone of the corbels, to the advantage of slabs bearing capacity. A few design equationsdeveloped for directly-supported R/C beams are used to predict the ultimate load in the case of dapped ends, and the fitting of the test results is very satisfactory. Finally, a recent strut-and-tie model is applied to evaluate the extra bearing capacity provided by the bending-up of the bottom longitudinal bars.

1. INTRODUCTION

The well-established use of R/C slabs or plates in the roofs of small-medium underground technical facilities or in temporary covers requires a proper design for the reinforcement, even if generally the service loads are rather limited (a more or less thick layer of soil, a bituminous layer or a water-proof lining often covered by a tiled floor).

In certain cases, however, like in the covers of underground facilities, severe loads cannot be ruled out in accidental situations, due – for instance - to the transit of a heavy vehicle when the building site is still open (Fig.1). (The maximum service load per axle is  120 kN according to the Italian Code for Highways, 2012, and142 kN according to AASHTO, 2010).

Because of slabs simple geometry (with rectangular shape and uniform thickness in most cases), straightforward restraints (simple supports along two opposite sides and unidirectional bending), simple bar layout (Fig.1) and moderate spans (2-4 m), however, the structural requirements are often underrated, and the reinforcement is often too light to the detriment of both durability and  safety, particularly in the case of shallow corbels running along the short sides.

Six 220x130 cm slabs featuring different bar layouts have been recently tested in Milan, in bending and shear. In the shear tests, the load was applied at 1/10 of the simply-supported span (210 cm), see Fig.2.

Slabs A1 andA2(Gambarova and Lo Monte, 2016, Tests 1-4 in bending and Tests 5-12 in shear) had longitudinal and transverse bar at the intrados, with the former

____________________________________

1Professor Emeritus, Politecnico di Milano pietro.gambarova@polimi.it

2PhD, MS Eng., Politecnico di Milano francesco.lo@polimi.it

3MS Eng. Student, Politecnico di Milano riccardovise@gmail.com

4MS Eng. Student, Politecnico di Milano matzec@hotmail.it

Figure 1. Possible accidental situations: (a) a heavy vehicle; and (b) a falling rock.

bars bent  up at their extremities; the  corbels were reinforced with hooks. Slabs B1 and B2 were reinforced with straight bars both at  the  intrados and at mid-depth(to reinforce also the corbels). In all four slabs the thickness was 15 cm, and the corbels had both the overhang and the depth equal to 10 cm. Slabs A1 and B1 were subjected to a shear load evenly distributed in the transverse direction, whilein Slabs A2 and B2 the load was rather concentrated in the transverse direction.

Slabs C and D (presented in this paper, Figs.2 and 3, Tests 13-16) have the same in-plane dimensions and simply-supported span, but the thickness is slightly larger (16 cm) and the corbels are slightly smaller (overhang and depth = 9 cm). The reinforcement is simpler than in Slabs A1/2 and B1/2, and the loads are evenly distributed in the transverse direction. Both Slabs C and D have a bottom net of straight bars, but Slab D has a second net of straight bars roughly at mid-depth (Fig.2a), and in Slab C the longitudinal bars of the second net are bent up to form hooks inside the corbels (Fig.2b).

The tests on Slabs C and D are aimed at (a) having fresh and direct information on slab behavior in shear (in terms of cracking and bearing capacity) for two simple but commonly used bar lay-outs; (b) checking the reliability of some of the design equations proposed in EC2(2004) and ACI (2008) codes for directly-supported R/C members – one-way slabs included – devoid of transverse reinforcement; and (c) investigating the extra-capacity of the same slabs, should the bottom longitudinal bars be bent-up to resist shear. With reference to the last point, a rathersimple strut-and-tie modeldeveloped by the first two authors is first recalled (Gambarova and Lo Monte, 2016) and then applied to the given slabs, in agreement with the available literature (Marti, 1985; Schlaich et al., 1987; Cook and Mitchell, 1988; Reineck, 2002; Reineck and Novak, 2010; Garber et al., 2014; Quinang et al., 2014) and code provisions (EC2, 2004; ACI, 2008).

Figure 2. Typical bar layouts found in one-way indirectly-supported R/C slabs:

(a) layout adopted in Slab C; and (b)  layout adopted in Slab D.

2. GEOMETRY, REINFORCEMMENT AND MATERIALS

The in-plan dimensions of the four slabs tested in this project a x b are 220 x 130 cm, and the thickness t is 160 mm. In the cantilevers (corbels) placed along the short simply-supported sides the depth tcrb and  overhang Lcrbare equal to 90 mm, Figs.2 and 3. The simply-supported span is 2100 mm in Tests 13 and 14 (Fig.3c) and 1900 mm in Tests 15 and 16 (Fig.3d). The bottom and mid-depth reinforcementsare the same in both slabs (98 and 128 + 712, respectively), as well as the transverse reinforcement (bottom and mid-depth: 28/200 mm). While  the  reinforcement of slab D consists of

Figure 3 – In-plan and lateral views of Slabs C and D, with uniformly-distributed load in the transverse direction.  L = 2100 mm, Tests 13 and 14 (a); L’ = 1900 mm, Tests 15 and 16 (b).

straight bars in both directions, in Slab C the corbels have a further set of hooks (712 hooks, whose depth is 66 mm and anchored length 500 mm (78 mm in the corbels and 422 mm in the thick part of the slab, Fig.2a). Neither slab is provided with transverse reinforcement in the disturbed zone (D-zone) between the corbel and the thick part of the slab; the hooks in the corbels are only meant to improve – by overlapping – the bond between the bottom longitudinal tensile bars of the corbels (712) and the concrete, as  the bonded length of the reinforcing bars in the corbels is rather short (90 mm, i.e. = 7-8max). As for the net cover of the bars, the nominal value was never smaller thanmax(12 mm).

Concrete and reinforcing steel are those commonly used in this kind of structural members (concrete C25: fck = 25 MPa and mean strength fc = 33 MPa; steel B 450 C: fyk = 450 MPa and mean strength at yielding fy = 520 MPa, measured on bar diameters equal to 6, 8, 10 and 14 mm).

The reinforcement ratio of the corbels crb, the effective depth of their section  dcrband the total area of their tensile bars Acrbare 1.67%, 64.3 mm and 1394 mm2, respectively. In the mid-span section the steel ratio l , the effective depth of the section d and the total area of the tensile bars Alare1.74%, 81.8 mm and 1846 mm2, respectively.

3.  LOADS AND INSTRUMENTATION

The aim of the tests was (a) to check slabs behaviors in shear under the ultimate loads (own weight + variable load, the latter amplified by 50%, i.e. 1.5 x 60 = 90 kN),   applied at  10% of the simply-supported span (Fig. 3 and Table 1); and (b) to investigate slabs response up to failure.

As shown in Fig.3, the load was cross-wise distributed over a 1300 x 60 mm2(2.8% of the total surface), the total surface, in order to have the pressure on the slab equal to 80 N/cm2 (max. allowed by the Italian code [1]). As shown in Figs.4a,b concerning two typical tests, the load was applied by means of a hydraulic jack (capacity 1000 kN) acting on very stiff spreaders consisting of rail stumps (length = slab width = 1300 mm).

In all the tests, steel and neoprene strips were inserted between the rail stump and the slab to apply the load exactly over the nominal surface (1300 x 60 mm) and to make the contact with the concrete as uniform as possible. The supports consisted in 40-mm steel bars; between these bars and the corbels a thick steel band and a neoprene strip

Table 1 – Summary of test results (Tests No. 13-16).

| Test No. | Slab | Reinf. | Load type | Test type | Test mode | Pmax [kN] |
| --- | --- | --- | --- | --- | --- | --- |
| 13/C1 | C | HKS | UDL | Shear | PLS | 125.0 |
| 14/C2 | C | HKS | UDL | Shear | PLS | 132.0 |
| 15/D1 | D | STR | UDL | Shear | PLS | 114.0 |
| 16/D2 | D | STR | UDL | Shear | PRT | 78.4 (*) |

HKS/STR = hooks/straight bars in the corbels

UDL = uniformly-distributed load in the cross-wise direction

PLS = complete load-displacement curve (loading branch + softening)

PRT = preliminary test aimed to check the behavior of the loading set-up

(*) Teststopped at roughly 70% of the expected maximum because of press malfunctioning

were placed, the latter being necessary to equalize concrete roughness along the bottom face of the corbels.

All tests were displacement controlled (displacement rate of the piston of the hydraulic jack = 0.025 mm/s). After a pre-loading cycle up to 15 kN (roughly 40% of the first-cracking load), the load was increased by 10-15 kN at a time up to 90 kN. Later, the tests were continued up to the load peak (Pmax) and beyond, and were stopped once the load had decreased by 20% compared with the peak load.

The tests were monitored by means of two sets of three medium-stroke LVDTs placed under the specimen along the unsupported sides; a 7th LVDT was placed under the centroid of the loaded area. Two sets of three short-stroke LVDTs were arranged astride the bisectors of the internal angles of the corbel closest to the applied load (Fig.4b). Finally, two further short-stroke LVDTs were mounted at the extremities of the corbel closest  to the applied load (Fig.4a) to measure the settling of the neoprene strip.

| (a) | (b) |
| --- | --- |

Figure 4 - Typical test: (a) detail of a simply-supported short side (east side; the longer north side is in the forefront); and (b) instrumentation placed across

the possible crack pattern (south-west corner).

4.  LOAD-DISPLACEMENT DIAGRAMS

The load-displacement diagrams (with the displacement measured under the centroid of the load) are plotted in Figs.5a,b. In all diagrams, the values of the displacements were cleared of the settlings exhibited by the neoprene strips along the short sides. One may note:

(a)	In Slab C (straight bars at the bottom and at mid-depth, with hooks in the corbels): Tests C1 and C2 denote a highly-repeatable behavior (Fig.5a), with the same initial stiffness, followed by very similar loading branches up to the peak load; even the peak - or maximum - loads are very close (125 and 132 kN).

(b)	In Slab D (straight bars at the bottom and at mid-depth, even in the corbels devoid of any hook): Tests D1 and D2 exhibit the same regular behavior (Fig.5b) up to 70% of the expected maximum load; above this load level, however, Test D1 proceeds regularly up to the peak load (114 kN), while the preliminary test D2 shows a sort of plateau (not indicated in Fig.5b), because of a malfunctioning of the press; the very good agreement up to 70% of the maximum load - and in general - between nominally-identical tests (see Tests C1 and C2) allow to conclude that Test D1 can be considered as fully representative of the corbels without hooks.

(c)    The initial stiffness and the general behavior up to roughly 2/3 of the maximum load are non affected by the hooks, as cracking at the inner corners of the corbels is either nil or very limited (see next section).

(d)   The peak load is improved by the hooks, as the average peak load measured in Tests C1 and C2 (128.5 kN, with hooks in the corbels) is 12-13% higher than that measured in Test D1 (114 kN, no hooks in the corbels); the reason may be the better reinforcement-concrete bond in the corbels of Slab C, where the hooks exert also a confining action on the concrete.

Figure 5.  Load-displacement diagrams: (a) Slab C, Test C1, west corbel (thin curve) and Test C2, east corbel (thick curve); and (b) Slab D, Test D1, east corbel (thin curve) and Test D2, west corbel (thick curve); the displacement is measured at 1/10 of the span.

5. CRACK PATTERNS

In both Slabs C and D the lack of transverse reinforcement (which may be introduced just by bending-up the straight longitudinal bars placed at the bottom of the slab) favor the formation of an arch-and-tie mechanism, as indicated by the rather shallow crack radiating from the inner corner of each corbel (Figs.7a,b). Providing hooks in the corbel (as in Slab C) affects neither the crack pattern nor the behavioral mechanism.

As for the cumulative crack opening at the inner corners of the corbels, as a function of the applied load, there are no major differences between Slab C (with hooks in the corbels, Fig.7a) and Slab D (without hooks, Fig.7b) at least up to 70% of the maximum expected load, but it is fair to say that the dispersion of the experimental results is rather

high (see in Figs.7b,c how cracks open earlier in Test C1 compared with Test C2).

| Figure 6a. Slab C with hooks, Test C2, north corbel; Pmax = 132.0 kN . | Figure 6b - Slab D without hooks, Test D1, north corbel; Pmax = 114.0 kN. |
| --- | --- |

Figure 7. Cumulative crack width at inner corners: (a) Slab D, west corbel, north side;

(b) Slab C, west corbel, north side; and (c) Slab C, east corbel, south side.

6.  NUMERICAL EVALUATION OF THE BEARING CAPACITY IN SHEAR

The rather flat cracks in the discontinuity zone between the corbel and the full slab (Fig.6) indicate the formation at the ultimate limit state of a shallow-arch and tie mechanism, similarly to what occurs at the extremities of a directly-supported transversely-unreinforced R/C beam having an effective depth equal to dcrb(Fig.7b). On the contrary, should the bottom longitudinal reinforcement be bent-up in the form of a hook, the 40-45° cracks would indicate the formation of a much more efficient truss mechanism(or strut-and-tie mechanism), as in Fig.7a.

Investigating the advantages brought in by bending-up the bottom reinforcement is – therefore – quite interesting, even if neither of the two tested slabs had bent-up bars.

Figure 7. Simplified behavior of dapped ends:  (a) strut-and-tie system to model hooks and bent-up bars; and (b) shallow-arch and tie system to model straight bars.

6.1 Application of the design equations valid for directly-supported R/C beams

The shear capacity VR (that is equal to the reaction Ru at the support, see Figs.3a,b) is evaluated by means of the equations for R/C beams devoid of shear reinforcement provided by ENV 1992-1-1 (1992), EN 1992-1-1 (2004) and ACI (2008; Eq.11-5 in ACI 318M-08); in other words, reference is made to a R/C beam having the same section of the corbel (effective depth dcrb effective depth of the slab d):

ENV (1992):

VR = R k (1.2 + 40 crb) bw dcrb = 0.54x1.536 x (1.2 + 40x1.67%)x1300x64.3 =

= 129.5 kN                                                                                                                                    (1)

EN (2004):

VR = CRd,c k (100 crb fc)1/3bw dcrb = 0.18x2.0^ or 2.76^^x3.81x1300x64.3  =

= 114.7^ or 158.2^^ kN                                                                                                               (2)

ACI (2008):

VR = [0.16 fc1/2 + 17 crb(Vu dcrb/Mu,crb)] bw dcrb =

= [0.16 x 331/2 + 17 x 1.67% / 0.563] x 1300 x 64.3 = 119.1 kN                                             (3)

where: dcrb(corbel effective depth) = 64.3 mm****; bw (section width) = 1300 mm;

d (slab effective depth) =  81.8 mm

R (mean shear strength) = 0.54 MPa *; k (size-effect parameter) = 1.6 - d (m) =

=  1.6 - 0.0643 = 1.536;

crb(% of the bottom reinf. of the corbel) = Acrb/(bw dcrb) = 1394/(1300x64.3) = 1.67%

As from Figs.3c,d, the following simple relationships hold for the reaction at the support R (= Vmax) and the load P:

R = pL/2 + 0.9 PorP = 1.11 (R – pL/2) = 1.11 (Vmax – pL/2)(4a,b)

where p (own weight per unit length) = 5.10 kN/m; L (simply-supported span) = 2.1 m.

At the ultimate limit state:

Pu =  Pmax= 1.11 (VR – pL/2) = 1.11 (Vmax – pL/2)                               (5)

Hence, the values of P u are:

ENV: Pu  = 137.8 kN ; EN: Pu  = 121.4/169.7 kN ; ACI: Pu = 126.3 kN             (6)

In Eq.1, the value R = 0.54 MPa comes from the value 0.30 MPa specified by ENV for concrete grade C25/30 in the design at the ultimate limit state; then 0.30 MPa must be multiplied by  c = 1.5 and the characteristic strength fck = 25 MPa must be replaced with the mean strength fc = 33 MPa, on the basis of the ratio (fc/fck)2/3 = (33/25)2/3 = 1.20:  τR = 0.30 x 1.5 x 1.20 = 0.54 MPa.

In Eq.2, fck = 25 MPa was replaced with fc = 33 MPa; c was given a unit value; the factor k = [1 + (200/dcrb)1/2] was given its full value 2.76 (^^) or was limited to 2.0 (^), as indicated in EN (2004); dcrb should be introduced in mm.

In Eq.3, to introduce the sectional discontinuity between the corbel and the slab, the ratio (Vu dcrb/Mu,crb) should be taken equal to (tcrb/t) = 90/160 = 0.563.

The agreement between the numerical predictions based on codes (Pu = 137.8, 121.4/ /169.7 and 126.3 kN) and the experimental values (Pmax = 127.5 kN, mean of the two nominally-identical Tests C1 and C2 - corbels with hooks - is rather satisfactory.The equation provided by ACI (2008), however, has an edge over the other equations, if the ratio (Vu d/Mu) is introduced as suggested in this paper (but it is still an open question).

6.2 Extra bearing capacity provided by bending up the longitudinal reinforcement

The discontinuity zone including the corbel and the region of the slab closest to the corbel (and up to the axis CE of the concentrated load) can be studied by means of strut-and-tie systems (Fig.8) in the case of a simply-supported beam or unidirectional slab, subjected to a concentrated load P and to the own weight p. In Fig.8, the load is represented by the reaction R at the support (Eq.4). The positions of Joints A, B, C, D and E can be determined easily from geometry. Note that for the depth of struts section the value ¼ of the thickness of the slab is commonly adopted.

As for Joint F, several choices are possible, depending on the adopted strut-and-tie system and on the  profile assumed for the bond stresses acting at the interface between the bottom reinforcement of the corbel (Tie AF) and the concrete (L in Figs.8b,c). In principle, any point along the bonded length is equally acceptable for the position of Joint F, but a reasonable choice may be the point where the resultant of the bond stresses is applied (coordinate x”, Fig.8b, for a uniform bond-stress distribution).

Figure 8 – Strut-and-tie systems for the D-zone between a corbel and a slab ( = 40°).

In all cases of Fig.8, Tie AF transfers its axial force NAF (= N0) to the concrete via bond, with a sizable effect on the local behavior in System I and no effect in System IV. In System I the position of F comes from equilibrium on condition that all struts are in compression or stress-free. In System IV the position of point F is immaterial and does not affect the local behavior (the alignement along CE is just for convenience).

There is, however, a further question: is the axial force NAF entirely transmitted to the struts FB and FD (Systems I and II), or a share of NAF is transmitted via adhesion to the thick part of the slab, far from the discontinuity zone? In the first case NAF overloads the ties BD and DE, and in the second case a more or less sizable share of NAF is transmitted to the slab (100% and 50% in Systems IV and III, respectively).

The actual behavior of Tie AF is halfway between those of Systems II and IV. Thanks to the rather long anchored length of the horizontal arms of the hooks reinforcing the corbels, one may assume that a share  NAF be transferred to the discontinuity region via Struts BF and DF, and the remaining share (1 - ) NAF be transferred to more distant regions (System III). Note that in Fig.8c, x” is the coordinate of the centroid of the bond stresses resisted by BF and DF, and may be a good guess for the position of Joint F. For any given value of x’ (and for the corresponding position x” of Joint F) and for any assumed bond-stress distribution (uniform, linear or parabolic), it is possible to identify the share  (= allotment factor) of the axial force NAF, and the position x” of Joint F (through η = x”/L = position factor), as a function of  = x’/L (= efficiency factor); for a uniform distribution of the bond stresses,  and are very simple functions of  (Gambarova and Lo Monte, 2016):

=  and  = ½   for B(x) = o                                (7)

where x is the coordinate along the bonded arm of the hook measured from the discontinuity section.

Within limit analysis, by writing the equilibrium equations for System III (for any value of ) and by imposing in turn the yielding of the ties AF, BD and DE (Fig.9), an  envelope  is  obtained,  whose  maximum (= bearing capacity) is  associated with the simultaneous yielding of Ties BD and DE. The values of the parameter   are:

= 0.394/0.638/0.818 for uniform/linear/parabolic distribution of the bond stresses

while  = x’/L = 0.394/0.398/0.433, and η = x”/L = 0.197/0.183/0.178, respectively.

The linear profile of the bond stresses along the bottom arm of the hooks provides the best estimate of the load-bearing capacity (000.0 kN) while uniform/parabolic profiles lead to over/under-evaluations (000.0 and 000.0 kN, respectively). Systems I and IV (Fig.8) yield lower and upper bounds, respectively, for the bearing capacity.

Figure 9. Plots of the ultimate loads Pu’, Pu” and Pu”’ (associated with the yielding of Ties AF, BD and DE), and of the efficiency and position factors,  and , for a linear profile of the bond stresses acting along the bottom arm of the corbel; (o) =bearing capacity of the corbel.

Summing up, improving the details of the bottom bars, by bending them up to form extended hooks in the thick part of the slab increases dramatically the bearing capacity in shear, as demonstrated by the following numbers:

- Straigth bars in the slab and in the corbels: Pu= 114 kN;

- Straight bars in the slab and hooked bars or hooks in the corbels: Pu = 127.5 kN;

- Bent-up bars in the slab and hooked bars or hooks in the corbel:  Pu = 000.0 kN.

7.  CONCLUDING REMARKS

Two rather usual rectangular uni-directional  lightly-reinforced slabs simply-supported along the short sides by means of corbels (dapped ends) have been experimentally investigated in the 2nd phase of a project concerning six slabs. All the corbels were tested in shear. The aim was to check their ultimate behaviors for different reinforcement layouts (with/without hooks in the corbels and bent-up extremities in the longitudinal bars). The four tests in shear presented in this paper and the numerical evaluations lead to the concluding remarks listed below.

- Past the working loads, cracks start radiating at 40-45° from the internal corners of the corbels, and later remain rather flat towards the loads, in agreement with the mechanisms based on shallow arches provided with ties or chains.

- The hooks in the corbels, accompanied by straight bars at the bottom and at mid-depth of the slab, slightly increase the bearing capacity, by helping the poorly embedded longitudinal bars (short bonded length and small net cover in the corbels, even if under the positive action of the lateral pressure exerted by the support).

- The design-oriented equations introduced for transversely-unreinforced R/C beams predict rather well the bearing capacity of the dapped ends devoid of shear reinforcement, provided that the sectional discontinuity be properly introduced.

- Bending up the bottom longitudinal bars and providing their extremities with hooks more than doubles the bearing capacity in shear, as demonstrated by a simple strut-and-tie model, which requires (a) a proper definition of the joints based on the profile of the bond stresses along the arms of the hooks; and (b)the introduction of the share of the pull-out force of each hook, which isresisted by the strut-and-tie system.

8.  ACKNOWLEDGEMENTS

The experimental campaign was financially supported by a firm active in the construction and management  of waste-water treatment plants, whose headquarters are located in Northern Italy. The test results were presented at the workshop “Durability and Sustainability of Concrete Structures” organized by ACI – Italy Chapter, 1-3 October 2015 (Bologna, Italy).

9.  REFERENCES

AASHTO (2010). Bridge Design Specifications – Clause 3.6.1.2, 5th Edition.

ACI 318M–08 and Commentary (2008). Building Code Requirements for Structural Concrete, Chapter 11 “Shear and Torsion”, and Appendix A “Strut-and-Ties Models”, 379-394.

Cook W.D. and Mitchell D. (1988). “Studies of Disturbed Regions near Discontinuities in Reinforced-Concrete Members”, ACI Structural J., V.85, No.2, 206-216.

ENV-1992-1-1 (1992). Design of  Concrete Structures - Part 1-1: General Rules and Rules for Buildings.

EN 1992-1-1 (EC2, 2004). Design of Concrete Structures – Part 1-1, Chapter 6.5 “Design by means of Strut-and-Tie Models”.

Gambarova P.G. and Lo Monte F. (2016). “Design Issues about the Bar Lay-Out at the Dapped Ends of Simply-Supported One-Way R/C Slabs”. Proc. Int. Conf. on “Concrete under Severe Conditions – CONSEC 2016”, September 12-14, Lecco (Italy), 8 pp., in press.

Garber D.B., Gallardo J.M., Huaco G.D., Samaras V.A. and Breen J.E. (2014). “Experimental Evaluation of Strut-and-Tie Model of Indeterminate Deep Beams”, ACI Structural J., V.111, No.4, 873-880.

Italian Code for Highways (2012). Limit Mass – Clause 62. Ministerial Decree, January 24, 2012, No.1.

Marti P. (1985). “Basic Tools of Reinforced Concrete Beam Design”, ACI Journal, No.82-4, January-February 1985, 46-56.

Qinang Hu, Tyler Ley M. and Russell B.W. (2014). “Determining Efficient Strut-and-Tie Models for Simply Supported Beams Using Minimum Strain Energy”, ACI Structural J., V.111, No.5, 1015-1026.

Reineck K.H. (Ed., 2002), and Reineck K.H. and Novak (eds., 2010). “Examples for the Design of Structural Concrete with Strut-and-Tie Models”, ACI SP-208, 242 pp.; SP-273, 288 pp.

Schlaich J., Schäfer K. and Jennewein M. (1987). “Toward a Consistent Design of Structural Concrete”, Special Report, PCI Journal, May-June 1987, 75-150.